## Slide 1: Industrial Pharmacy II Assist. Lect. Amenah M. M.

## Slide 2: Sugar Coating

## Slide 3: The sugar coating process involves several steps, the duration of which ranges from a few hours to a few days. A successful product greatly depends on the skill of the coating operator.

## Slide 4: This is especially true in the pan-ladling method, in which the coating solutions are poured over the tablet cores. The operator determines 1. The quantity of solution to add. 2. The method and rate of pouring. 3. When to apply drying air. 4. How long or how fast the tablets should be tumbled in the pan.

## Slide 5: Newer techniques utilize spraying systems and varying degrees of automation to improve coating efficiency and product uniformity. Regardless of the methods used, a successful sugar coating process yields elegant, highly glossed tablets.

## Slide 6
The basic sugar coating process involves the following steps:
1. Sealing.
2. Sub-coating.
3. Syruping (Smoothing).
4. Finishing.
5. Polishing.

## Slide 7: The tablet cores preferably have deep convex surfaces with thin rounded edges to facilitate sugar coating. Since sugar coating tends to be long and vigorous, the cores should be relatively resistant to breakage, chipping, and abrasion.

## Slide 8: 1. Seal Coating
To prevent moisture penetration into the tablet core, a seal coat is applied. This is especially needed in pan-ladling processes, in which localized over-wetting of a portion of the tablet bed occurs.

## Slide 9: Without a seal coat, the overwetted tablets would absorb excess moisture, leading to tablet softening or disintegration and affecting the physical and chemical stability of the finished product.

## Slide 10: In spray processes, it is possible to adjust the application of the sub-coats and further coats so that localized over-wetting does not occur. This adjustment thus eliminates the seal coating step.

## Slide 11: Shellac is an effective sealant, but tablet disintegration and dissolution times tend to lengthen on aging because of the polymerization of the shellac.

## Slide 12: Zein is an alcohol-soluble protein derivative from corn that has also been used as an effective sealant. Lengthening dissolution times have not been reported on aging of zein seal coated tablets.

## Slide 13: 2. Subcoating
The subcoating is applied to round the edges and build up the tablet size. Sugar coating can increase the tablet weight by 50 to 100%. The subcoating step consists of alternately applying a sticky binder solution to the tablets followed by a dusting of subcoating powders and then drying.

## Slide 14: Subsequent subcoats are applied in the same manner until the tablet edges have been covered and the desired thickness is achieved.

## Slide 15: For spray processes, a subcoating suspension containing both the binder and the insoluble powder is sprayed intermittently on the tablet bed. With both methods of application, control of the drying rate is critical to obtaining a rapid application of the subcoat.

## Slide 16: 3. Syrup (Smoothing/Color) Coating
The purpose of this step is to cover and fill in the imperfections in the tablet surface caused by the subcoating step, and to impart the desired color to the tablet. This step perhaps requires the most skill.

## Slide 17: The first syrup coats usually contain some suspended powders and are called "grossing syrups" Dilute colorants can be added to this phase to provide a tinted base that facilitates uniform coloring in later steps.

## Slide 18: In general, no color is added until the tablets are quite smooth; premature application to rough tablets can produce a mottled appearance in the final coated tablets.

## Slide 19
In subsequent syruping steps, syrup solutions containing the dye are applied until the final size and color are achieved. In the final syruping or finishing step, a few clear coats of syrup may be applied.

## Slide 20: 4. Polishing
The desired luster is obtained in this final step of the sugar coating process. The tablets can be polished in clean standard coating pans, or canvas-lined polishing pans, by carefully applying powdered wax (beeswax or carnauba) or warm solutions of these waxes in naphtha or other suitable volatile solvents.

## Slide 21
Film Coating

## Slide 22: Since film coating originated from the pan sugar coating process era. With the possible exception of the air suspension coater, film coating and sugar coating share the same equipment and process parameters.

## Slide 23: Pan-Pour Methods
Coating compositions used in the earlier pan-pour methods were usually too viscous to be sprayed effectively. Tablets coated by pan-pour methods are subjected to alternate solution application, mixing and drying steps similar to pan-pour sugar coating.

## Slide 24: The method is relatively slow and relies heavily on the skill and technique of the operator to balance the steps to produce an acceptable product. Tablets that are film coated by pan-pour processes almost always require additional drying steps to remove latent solvents.

## Slide 25: Aqueous based film coatings are not suitable for this method of application because localized overwetting inherent with the pan-pour process causes numerous problems ranging from surface erosion to product instability due to unacceptably high latent moisture content in the cores.

## Slide 26: Pan-Spray Methods
Spraying lends versatility to the process and allows for automated control of liquid application. Spray patterns are selected to provide a continuous band across the tablet bed surface. Broad, flat spray patterns are usually chosen by selection of appropriate nozzle.

## Slide 27
Process Variables
Whether the coating process is in a conventional pan system or in one of the perforated pan systems previously described, certain elements of the process need to be controlled to ensure consistent product quality.

## Slide 28: The variables to be controlled in pan-spray film coating processes are: 1. Pan Variables Pan design/baffling, speed, pan load 2. Process Air air quality, temperature, airflow rate/volume/balance 3. Spray Variables spray rate, degree of atomization, spray pattern, nozzle-to-bed distance.

## Slide 29
Pan Variables
Pan shape, baffling, rotational speed, and loading all affect the mixing of the tablet mass. Uniform mixing is essential to depositing the same quantity of film on each tablet. The tablet coating adds an approximate increase in weight of only 2 to 5% to the tablet.

## Slide 30: Unacceptable color uniformity or enteric film integrity is encountered if the tablets are inadequately coated because of poor tablet movement in the coating pan.

## Slide 31: Materials Used in Film Coating
The coating materials may be a physical deposition of the material on the tablet substrate, or they may form a continuous film with a wide variety of properties depending upon the composition of the coating formulations.

## Slide 32: Examples of physical deposition of the coating materials are the techniques of sugar, shellac, and wax coatings.

## Slide 33
An ideal film coating material should have the following attributes:
1. Solubility in solvent of choice for coating preparation.
2. Solubility required for the intended use,. e.g ., free water-solubility, slow water-solubility, or pH-dependent solubility (enteric coating)
3. Capacity to produce an elegant looking product.

## Slide 34
4. Stability in the presence of heat, light, moisture, air, and the substrate being coated. The film properties should not change with aging
5. Essentially no color, taste or odor.
6. Compatibility with common coating solution additives:
7. Nontoxicity with no pharmacologic activity, and ease of application to the particles or tablets.

## Slide 35
8. Resistance to cracking, and provision of adequate moisture, light, odor, or drug sublimation barrier when desired.
9. No bridging or filling of the debossed tablet surfaces by the film former.
10. Ease of printing procedure on high-speed equipment.

## Slide 36
Compositions of Film Coating

## Slide 37
1. Film Formers
Nonenteric Materials
1. Hydroxypropyl Methylcellulose, USP.
2. Methyl Hydroxyethylcellulose.
3. Ethylcellulose.
4. Povidone, USP.
5. Sodium Carboxymethylcellulose, USP.
6. Polyethylene Glycols.
7. Acrylate Polymers. (Eudragit)

## Slide 38
Enteric Materials
Some of the most important reasons for enteric coating are as follows:
1. To protect acid-labile drugs from the gastric fluid, e.g., enzymes and certain antibiotics.
2. To prevent gastric distress or nausea due to irritation from a drug, e.g. , sodium salicylate.

## Slide 39
3. To deliver drugs intended for local action in the intestines, e.g ., intestinal antiseptics.
4. To deliver drugs that are optimally absorbed in the small intestine to their primary absorption site in their most concentrated form.
5. To provide a delayed-release component for repeat-action tablets.

## Slide 40
An ideal enteric coating material should have the following properties:
1. Resistance to gastric fluids.
2. Ready susceptibility to or permeability to intestinal fluids.
3. Compatibility with most coating solution components and the drug substrates.
4. Stability alone and in coating solutions. The films should not change on aging.

## Slide 41
5. Formation of a continuous (uninterrupted) film.
6. Nontoxicity.
7. Low cost.
8. Ease of application without specialized equipment.
9. Ability to be readily printed or to allow film to be applied to debossed tablets.

## Slide 42
Enteric Materials
Cellulose Acetate Phthalate (CAP).
Acrylate Polymers.
Hydroxypropyl Methylcellulose Phthalate.
Polyvinyl Acetate Phthalate

## Slide 43
2. Solvents
The primary function of a solvent system is to dissolve or disperse the polymers and other additives and convey them to the substrate surface.

## Slide 44
Some important considerations for an ideal solvent system are as follows
1. It should either dissolve or disperse the polymer system.
2. It should easily disperse other coating solution components into the solvent system.
3. Small concentrations of polymers (2 to 10%) should not result in an extremely viscous solution system (>300 cps), creating processing problems.

## Slide 45
4. It should be colorless, tasteless, odorless, inexpensive, nontoxic, inert, and nonflammable.
5. It should have a rapid drying rate (the ability to coat a 300 kg load in 3 to 5 hours).
6. It should have no environmental impact.

## Slide 46
The most widely used solvents, either alone or in combination are water, ethanol, methanol, isopropanol, chloroform, acetone, methylethylketone, and methylene chloride. Because of environmental and economic considerations, water is the solvent of choice; however, several polymers cannot be applied from aqueous systems.

## Slide 47
Drugs that readily hydrolyze in the presence of water can be more effectively coated with nonaqueous-solvent-based coatings. Such a process might require applying an initial sealing coat from an organic-based subcoating, followed by aqueous color and gloss coating.

## Slide 48
3. Plasticizers
The quality of a film can be modified by the use of "internal" or "external" plasticizing techniques. Internal plasticizing pertains to the chemical modification of the basic polymer that alters the physical properties of the polymer.

## Slide 49
Most often, the formulator uses external plasticizers as additives to the coating solution formula so that the desired effects are achieved for the film. An external plasticizer can be a nonvolatile liquid or another polymer, which when incorporated with the primary polymeric film former, changes the flexibility, tensile strength, or adhesion properties of the resulting film.

## Slide 50: The Choice of plasticizer depends upon; The ability of plasticizer material to solvate the polymer and alter the polymer-polymer interactions. When used in correct proportion to the polymer, these materials impart flexibility by relieving the molecular rigidity.

## Slide 51: The type of plasticizer(s) and its ratio to the polymer can be optimized to achieve the desired film properties.

## Slide 52: One should also consider the viscosity of the plasticizer; its influence on the final coating solution; its effect on film permeability, tackiness, flexibility, solubility, and taste; and its toxicity, compatibility with other coating solution components, and stability of the film and the final coated product.

## Slide 53: A combination of plasticizers may be needed to achieve the desired effect. The concentration of the plasticizers depends on many factors, including 1. The polymer chemistry. 2. Method of application. 3. The other components present in the system. 4. Changes in the drying rate or use of elevated temperatures may alter the influence of the plasticizer in the coating process.

## Slide 54: The presence of titanium dioxide, colorants, flavors, and other additives also affect the film former. Most film formers tolerate only a certain additive load, and beyond that limit, the film properties are adversely affected. Recommended levels of plasticizers range from 1 to 50% by weight of the film former.

## Slide 55: Some of the commonly used plasticizers are castor oil, propyleneglycol, glycerin, low-molecular-weight polyethylene glycols of 200 and 400 series, and surfactants. e.g., polysorbates (Tweens), sorbitan esters (Spans), and organic acid esters.

## Slide 56: For an external plasticizer to be effective, it should be soluble in the solvent system used for dissolving the film former and plasticizer. The plasticizer and the film former must be at least partially soluble or miscible in each other.

## Slide 57: 4. Colorants - Colorants may be soluble in the solvent system or suspended as insoluble powders. -They are used to provide distinctive color and elegance to a dosage form. -To achieve proper distribution of suspended colorants in the coating solutions requires the use of fine-powdered colorants (<10 microns).

## Slide 58: The most common colorants in use are certified (FD&C) or (D&C) colorants. These are synthetic dyes or lakes of dyes. Most commercially available lakes contain 10 to 30% of the pure dye content, but some lakes approach up to 50%.

## Slide 59: The concentration of colorants in the coating solutions depends on the color shade desired, the type of dye (dye versus the lake of the dye), and the concentration of the opaquant-extenders. If a very light shade is desired, a concentration of less than 0.01% may be adequate. On the other hand, if a dark color is desired, a concentration of more than 2% may be required.

## Slide 60: The inorganic materials (iron oxides) and the natural coloring materials (anthocyanins, caramel, carotenoids, chlorophyll, indigo, flavones, turmeric, and carminic acid) are also used to prepare coating solutions.

## Slide 61: 5.Opaquant-Extenders These are very fine inorganic powders used in the coating solution formulations to provide more pastel colors and increase film coverage. These opaquants can provide a white coating or mask the color of the tablet core.

## Slide 62: Colorants are much more expensive than these inorganic materials, and effectively less colorant is required when opaquants are used. The most commonly used material for this purpose is titanium dioxide. Some other materials are silicates (talc, aluminum silicate), carbonates (magnesium carbonate), sulfates (calcium sulfate), oxides (magnesium oxide), and hydroxides (aluminum hydroxide)

## Slide 63: 5. Miscellaneous Coating Solution Components Flavors or sweeteners are added to mask objectionable odors or to enhance a desired taste. Surfactants are used to solubilize otherwise immiscible or insoluble ingredients, or to facilitate faster dissolution of the coating.

## Slide 64: Antioxidants are incorporated to stabilize a dye system to oxidation and color change. Antimicrobials are added to prevent microbial growth in the coating composition during its preparation and storage, and on the coated tablets.

## Slide 65: Film Defects

## Slide 66: 1. Sticking and Picking. Overwetting or excessive film tackiness causes tablets to stick to each other or to the coating pan. On drying, at the point of contact, a piece of the film may remain adhered to the pan or to another tablet, giving a "picked" appearance to the tablet surface and resulting in a small exposed area of the core.

## Slide 67: A reduction in the liquid application rate or increases in the drying air temperature and air volume usually solve this problem. Excessive tackiness may be an indication of a poor formulation.

## Slide 68: 2. Roughness
A rough or gritty surface is a defect often observed when the coating is applied by a spray. Some of the droplets may dry too rapidly before reaching the tablet bed, resulting in deposits on the tablet surface of "spray-dried" particles instead of finely divided droplets of coating solution.

## Slide 69: Moving the nozzle closer to the tablet bed or reducing the degree of atomization can decrease the roughness due to "spray-drying."

## Slide 70: 3. Orange-Peel Effects
Inadequate spreading of the coating solution before drying causes a bumpy or "orange-peel" effect on the coating. This indicates that spreading is impeded by too rapid drying or by high solution viscosity. Thinning the solution with additional solvent may correct this problem.

## Slide 71
4. Bridging and Filling.
During drying, the film may shrink and pull away from the sharp corners of an intagliation or bisect, resulting in a 'bridging" of the surface depression. Increasing the plasticizer content or changing the plasticizer can decrease the incidence of bridging.
.

## Slide 72
Filling is caused by applying too much solution, resulting in a thick film that fills and narrows the monogram or bisect. In addition, if the solution is applied too fast, overwetting may cause the liquid to quickly fill and be retained in the monogram. Judicious monitoring of the fluid application rate and thorough mixing of the tablets in the pan prevent filling

## Slide 73
5. Blistering.
When coated tablets require further drying in ovens, too rapid evaporation of the solvent from the core and the effect of high temperature on the strength, elasticity, and adhesion of the film may result in blistering. Milder drying conditions are warranted in this case.

## Slide 74
6. Hazing/Dull Film.
This is sometimes called bloom. It can occur when too high a processing temperature is used for a particular formulation. Dulling is particularly evident when cellulosic polymers are applied out of aqueous media at high processing temperatures. It can also occur if the coated tablets are exposed to high humidity conditions and partial solvation of film results.

## Slide 75
7. Color Variation.
Improper mixing, uneven spray pattern, and insufficient coating may result in color variation. The migration of soluble dyes, plasticizers, and other additives during drying may give the coating a mottled or spotted appearance.

## Slide 76
The use of lake dyes eliminates dye migration. A reformulation with different plasticizers and additives is the best way to solve film instabilities caused by the ingredients.

## Slide 77
8. Cracking.
Cracking occurs if internal stresses in the film exceed the tensile strength of the film. The tensile strength of the film can be increased by using higher-molecular-weight polymers or polymer blends. Internal stresses in the film can be minimized by adjusting the plasticizer type and concentration, and the pigment type and concentration.

## Slide 78
Thank You